Poly-L Lysine Coating Slides

- Place glass slides into glass bottomless slide racks and place in a beaker

- Add an appropriate volume of 1M HCl (enough to cover the racks)

1M HCl = 86.2 ml in 1 liter

- Boil for 10 minutes

- Place beaker under steady stream of water until the slides are completely rinsed

- Dip each rack (1 at a time) into the poly-L lysine solution in a glass bowl for 10 minutes (400 ml)

Poly-L lysine solution:  50 (g/ml in 10 mM Tris pH 8 (0.02 g Poly-L lysine in 396 ml water and 4 ml 1M Tris  pH 8)

- Let slides dry on bench (make sure they are covered so nothing sticks to them)

- Place sides in a clean, covered slide rack